## Slide 1
Calculation of Area of Substrate, Substance and Spheres

## Slide 2: Interpretation Example
Given that our Area of Scan = 10цm * 10цm => 100цm2
From Cellpose plus, we extract
  Area of Spheres = 43.34 цm2
  Area of exclusively Substrate = 39.38 цm2
    (i.e. Area without substance)
  Area of Substance = (Total area of Scan – Area of exclusively substrate)
    Therefore = 100 – 39.38 = 61.62цm2
Therefore, the metric Ratio of
Area of Spheres/ Area of Substrate coated with Substance = 43.34/61.62
  = 0.703

## Slide 3: Area of Spheres, Substance & Substrate - Summarized
Sample | Area of Sphere (in um^2) | Area of Substrate(in um^2) | Area of Substance(in um^2)
A | 44.24 | 18.38 | 81.62
Б | 44.34 | 39.68 | 60.32
В | 12.25 | 9.79 | 90.21
Г | 32.81 | 0 | 100
Д | 7.42 | 0 | 100
Е | 3.34 | 0 | 100
Ж | 45.1 | 5.46 | 94.54
З | 3.91 | 0 | 100
И | 0 | 0 | 100
К | 43.23 | 3.34 | 96.66
Л | 24.74 | 0 | 100
М | 26.29 | 3.69 | 96.31
Н | 24.74 | 0 | 100
О | 0 | 5.82 | 94.18

## Slide 4: (А)- 156 – CHCl3 - 23ºC – 23ºC – 10-4M
Original Image
Gwyddion Mask
Masked % | 14.95
Mask Height Value (цm) | 5.496

## Slide 5: (А)- 156 – CHCl3 - 23ºC – 23ºC – 10-4M
Spheres
Substance
Area of Spheres = 44.24цm2
Area of Substrate = 18.38цm2

## Slide 6: (Б)- 156 – CHCl3 – 23ºC – 4ºC – 10-4M
Original Image
Gwyddion Mask
Masked % | 28.04
Mask Height Value (цm) | 16.91
(Б)- 156 – CHCl3 – 23ºC – 4ºC – 10-4M

## Slide 7: (Б)- 156 – CHCl3 – 23ºC – 4ºC – 10-4M
Spheres
Substance
Area of Spheres = 43.34цm2
Area of Substrate = 39.68цm2

## Slide 8: (В)- 156 – CHCl3 - 4ºC – 23ºC – 10-4M
Original Image
Gwyddion Mask
Masked % | 21.60
Mask Height Value (цm) | 5.04

## Slide 9: (В)- 156 – CHCl3 - 4ºC – 23ºC – 10-4M
Spheres
Substance
Area of Spheres = 12.25цm2
Area of Substrate = 9.79цm2

## Slide 10: (Г)- 156 – CHCl3 - 23ºC – 23ºC – 10-5M
Original Image
Gwyddion Mask
Masked % | 22.43
Mask Height Value (цm) | 24.82

## Slide 11: (Г)- 156 – CHCl3 - 23ºC – 23ºC – 10-5M
Spheres
Substance
Area of Spheres = 32.81цm2
Area of Substrate = 100цm2 or area of full substrate/spheres

## Slide 12: (Д)- 156 – CHCl3+H2O - 23ºC – 23ºC – 10-4M
Original Image
Gwyddion Mask
Masked % | 
Mask Height Value (цm) | 

## Slide 13: (Д)- 156 – CHCl3+H2O - 23ºC – 23ºC – 10-4M
Spheres
Substance
Area of Spheres = 7.42цm2
Area of Substrate = 100цm2 or area of full substrate/spheres

## Slide 14: (Е)- 156 – CHCl3+H2O - 23ºC – 23ºC – 10-5M
Original Image
Gwyddion Mask
Masked % | 
Mask Height Value (цm) | 

## Slide 15: (Е)- 156 – CHCl3+H2O - 23ºC – 23ºC – 10-5M
Spheres
Substance
Area of Spheres = 3.34цm2
Area of Substrate = 100цm2 or area of full substrate/spheres

## Slide 16: (Ж)- 156 – Toluene - 23ºC – 4ºC – 10-4M
Original Image
Gwyddion Mask
Masked % | 32.71
Mask Height Value (цm) | 32.150

## Slide 17: (Ж)- 156 – Toluene - 23ºC – 4ºC – 10-4M
Spheres
Substance
Area of Spheres = 45.1цm2
Area of Substrate = 5.46цm2

## Slide 18: (З)- 156 – Toluene - 23ºC – 23ºC – 10-5M
Original Image
Gwyddion Mask
Masked % | 18.71
Mask Height Value (цm) | 12.962
In this sample, I have applied Polynomial Plan Levelling with degree = 2

## Slide 19: (З)- 156 – Toluene - 23ºC – 23ºC – 10-5M
Spheres
Substance
Area of Spheres = 3.91цm2
Area of Substrate = 100цm2 or area of full substrate/spheres

## Slide 20: (И)- 159 – CHCl3 - 23ºC – 23ºC – 10-4M
Original Image
Gwyddion Mask
Masked % | 24.30
Mask Height Value (цm) | 26.69

## Slide 21: (И)- 159 – CHCl3 - 23ºC – 23ºC – 10-4M
Spheres
Substance
Area of Spheres = 0цm2
Area of Substrate = 100цm2 or area of full substrate/spheres

## Slide 22: (К)- 159 – CHCl3 - 23ºC – 23ºC – 10-5M
Original Image
Gwyddion Mask
Masked % | 31.78
Mask Height Value (цm) | 21.698

## Slide 23: (К)- 159 – CHCl3 - 23ºC – 23ºC – 10-5M
Spheres
Substance
Area of Spheres = 43.23цm2
Area of Substrate = 3.34цm2

## Slide 24: (Л)- 159 – Toluene - 23ºC – 23ºC – 10-4M
Original Image
Gwyddion Mask
Masked % | 15.89
Mask Height Value (цm) | 17.00

## Slide 25: (Л)- 159 – Toluene - 23ºC – 23ºC – 10-4M
Spheres
Substance
Area of Spheres = 24.74цm2
Area of Substrate = 100цm2 or area of full substrate/spheres

## Slide 26: (М)- 159 – Toluene - 23ºC – 23ºC – 10-5M
Original Image
Gwyddion Mask
Masked % | 23.36
Mask Height Value (цm) | 9.139
In this sample, I have applied Polynomial Plan Levelling with degree = 2, since there are too many horizonal scratches

## Slide 27: (А)- 156 – CHCl3 - 23ºC – 23ºC – 10-4M
Spheres
Substance
Area of Spheres = 26.29цm2
Area of Substrate = 3.69цm2

## Slide 28: (Н)- 159 – CHCl3 - 23ºC - 4ºC – 10-4
Original Image
Gwyddion Mask
Masked % | 14.02
Mask Height Value (цm) | 14.41

## Slide 29: (А)- 156 – CHCl3 - 23ºC – 23ºC – 10-4M
Spheres
Substance
Area of Spheres = 24.74цm2
Area of Substrate = 100цm2 or area of full substrate/spheres

## Slide 30: (О)- 159 – CHCl3 - 4ºC – 23ºC – 10-4M
Original Image
Gwyddion Mask
Masked % | 17.76
Mask Height Value (цm) | 62.02

## Slide 31: (А)- 156 – CHCl3 - 23ºC – 23ºC – 10-4M
Spheres
Substance
Area of Spheres = 0 цm2
Area of Substrate = 5.82цm2